

**Product Overview:**

Baraf-S 3.5g is a high performance thermal paste that enhances the efficiency of heat conduction. Easy to apply and perfectly fills between your cooler and CPU. Comes with spreader.

**Specifications**

|  |  |
| --- | --- |
| **Model** | **Baraf-S 3.5g** |
| Thermal Conductivity | >5.15 W/m-K |
| Thermal Impedance | <0.004 ℃-in2/W |
| Specific Gravity | >3.25 |
| Viscosity | 12500 |
| Moment Beared Temperature | -50~340℃ |
| Operation Temperature | -30~280℃ |
| **Ingredients** | |
| Silicone Compounds | 10% |
| Carbon Compounds | 45% |
| Metal Oxide Compounds | 45% |
| **Weight** | |
| Net Weight | 3.5g |

**Warranty**

1 year

**Features**

* High performance thermal grease.
* Includes Spreader.

**Package Information**

|  |  |  |  |
| --- | --- | --- | --- |
| **Product Name** | **Product Number** | **EAN CODE** | **UPC CODE** |
| Baraf-S 3.5g | ACTG-NA24210.01 |  |  |
|  |  |  |  |
| **Carton Size ( L x W x H )** | 558 x 470 x 320 mm | **Carton Weight** | N.W 4.5 kg / G.W 5 kg |
| **Retail Box Size ( L x W x H )** |  | **Retail Box Weight** |  |
| **Carton Qty** | 1000 pcs | **Pallet Qty** | 24000(GP) / 28000(HQ) |
| FTP for pictures download: | | | |